## Slide 1: Mechanical Failure: Test Methodology and Diversification of Module Design/ Type and Affordable Insurance premium
SUN Meet
International Solar Alliance
18th November 2020
Dr. O. S. Sastry
Former Director General (NISE)

## Slide 2: Reasons for Occurrence of Mechanical failures in Solar Photovoltaic(SPV) Modules
Selection of BoM and Fabrication Process
Selection of Supersaturate (Glass), Wafer Thickness, EVA, Tadlar, Frame, etc.
Effect of Environmental Stress Temp, Humidity, Sand/dust
Installation, Handling and Transportation of SPV Modules
Wind Gust Effect , Ice deposition
Impact due to Stone , Hail, and other objectives, even Vandalism
Natural Calamities Cyclones, Fire Accidents , Earth Quakes

## Slide 3: Effect of Mechanical Failures in Modules
Performance Reduction [Yields, PR]
Safety Failures (Voltage, Breakage Risks)
Reduction in Performance Life (<25 Years)
Warranty/ Guarantee service contracts/ Agreements

## Slide 4: Selection of BoM and Fabrication Process
Selection of Supersaturate (Glass), Wafer Thickness, EVA, Tadlar, Frame, etc

## Slide 5: PV Module Structure

## Slide 6: Transportation of PV Modules

## Slide 7: IEC 62759-I: Transportation of PV Modules
Reasons for claims on PV modules (in total 2 million glass/foil and glass/glass modules) in the period 2006-2010.
Source: IEA-PVPS Task 13: „Review of Failures of Photovoltaic Modules“ Report IEA-PVPS T13- 01:2014
Failure rates based on 1310 thinfilm PV modules (frameless glass/glass modules) of plant operator juwi
Source: http://www1.eere.energy.gov/solar/pdfs/pvrw2010_p oster_collins.pdf

## Slide 8: IEC 62759: Transportation of PV Modules
Mishaps during
Transport
Module Packaging

## Slide 9: Maintaining Practices of PV Module Arrays - Bad Examples
Not to stand on the top module
Array - Create Micro-cracks
Not clean during the SUNNY hours of day
Create Hot Spots

## Slide 10: IEC 62759: Transportation of PV Modules
13 Modules
10 for transportation test
3 as reference

## Slide 11: IEC 62759: Transportation of PV Modules
Released in March 2016
Both is tested: Modules and packaging as a union
No pass/fail criterion

## Slide 12: Effect of Wind and Ice on PV Modules IEC 61215: 2016 /IEC TS 62782

## Slide 13: Wind Gust Effect (Dynamic Mechanical Load Test : 2400 pa)

## Slide 14: Wind Gust Effect (2400 pa):
Chart: Mechanical Load Test for Wind flow
| 0 | 0 | 1 | 1 | 1 | 2 | 2 | 2 | 3 | 3 | 3 | 4 | 4 | 4 | 5 | 5 | 5 | 6 | 6
Wind Load (Pa) | 0 | 2400 | 2400 | 0 | -2400 | -2400 | 0 | 2400 | 2400 | 0 | -2400 | -2400 | 0 | 2400 | 2400 | 0 | -2400 | -2400 | 0

## Slide 15: IEC TS 62782: Cyclic (Dynamic) Mechanical Load Test Sequence

## Slide 16: Snow Load Effect: (Static Mechanical Load Test: 5400pa)

## Slide 17: Snow Load Effect: (Mechanical Load Test)
Chart: 
| 0 | 0 | 1 | 1 | 1 | 2 | 2 | 2 | 3 | 3 | 3 | 4 | 4 | 4 | 5 | 5 | 5 | 6 | 6
Snow Load (Pa) | 0 | -2400 | -2400 | 0 | 2400 | 2400 | 0 | -2400 | -2400 | 0 | 2400 | 2400 | 0 | -2400 | -2400 | 0 | 5400 | 5400 | 0

## Slide 18: IEC TS 62782: Cyclic (Dynamic) Mechanical Load
TS = Technical specification, released in March 2016
No pass / fail criterion
“Stand alone TS but it is likely to be used in conjunction with other test standards… …other stress tests (HF, TC)…”
Mechanical Load Test Equipment

## Slide 19: IEC TS 62782: Cyclic (Dynamic) Mechanical Load Example: Two Module Designs
1000 Pa
IEC 61215
2400 Pa
0.0
-0.5
-1.0
-1.5
-2.0
power loss [%]
1000 Pa
IEC 61215
2400 Pa
800
600
400
200
0
cracks [-]

## Slide 20: Other Failure Effects on PV Modules IEC 61215: 2016

## Slide 21: Impact of Stone, Golf balls, hail,

## Slide 22: Hail Impact Tester

## Slide 23: BURNING SPOTS
INITIAL STAGE OF BURNING SPOT
FINAL STAGE AFTER FLARE
FRONT SIDE
OF MODULE
BEFORE
AFTER

## Slide 24: Techniques Available to Identify the failures in Modules
Electro Luminescence method (EL)
Infra Red Thermal Imaging of PV Modules
On site I-V measurements
Dry Hi-Pot and Wet Hi-pot tests of sample modules on site
Regular monitoring through SCADA
Carefully follow regular inspection tests as per IEC 62246

## Slide 25: Look While You Load
EL Camera
IV (other vendor)

## Slide 26: How to Mitigate Risk of Mechanical Failures in Modules
Selection & Certification of the Modules as per site conditions and quality plus criterion
On-site Checks using EL, I-V, IR & Hi-Pot verification of quality before installation
Follow regular inspection tests as per IEC 62246
Warranty/ Guarantee service contracts/ Agreements

## Slide 27: Thank you for Your Attention!!